High pressure torsion of Cu–Ag alloys at room temperature and 77 K

Boris Straumala, Askar Kilmametova, Petr Straumala, Brigitte Baretzkya

aInstitute of Nanotechnology, Karlsruhe Institute of Technology, Hermann-von-Helmholtz-Platz 1, 76344 Eggenstein-Leopoldshafen, Germany

aboris.straumal@kit.edu

The high-pressure torsion (HPT) of binary copper alloys with 8 and 12 wt. % Ag has been studied at two different temperatures THPT, namely at room temperature (300 K) and at the boiling temperature of liquid nitrogen (77 K). Before HPT, the Cu–Ag alloys have been annealed at two different temperatures of 500 and 780 °C. Thus, before HPT the studied alloys consisted of Ag-particles in the Cu-based matrix with silver content cinit from almost zero to 8 wt.%. After about 1.5 plunger rotations a certain steady-state concentration css of the alloying element is reached in the matrix. It is determined by the dynamic equilibrium between the rate of defects production and defects relaxation (annihilation) during HPT. The css was measured in our experiments using the dependence of lattice constant in copper-based solid solution on the silver concentration. css was different for different THPT. For THPT = 300 K the css value was about 5.5 wt. % Ag. It coincides with the value observed previously in [1]. The css = 5.5 wt. % Ag is equal to the solubility of silver in copper at 700 °C. For THPT = 77 K the css value was about 4.0 wt. % Ag. The css = 4.0 wt. % Ag is equal to the solubility of silver in copper at 600°C. Thus, the decrease of THPT from 300 K to 77 K leads to the decrease of the steady state concentration. The observed phenomenon is discussed using the ideas of non-equilibrium thermodynamics of open systems. During HPT the decomposition of a solid solution competed with dissolution of precipitates. As a result, a dynamic equilibrium established between precipitation and dissolution at steady-state deformation stage. In this dynamic equilibrium a certain steady-state concentration css of the alloying element is reached in the matrix.

Keywords: high-pressure torsion, deformation temperature, steady-state.

References:

[1] B.B. Straumal, A.R. Kilmametov, B. Baretzky, O.A. Kogtenkova, P.B. Straumal, L. Lityńska-Dobrzyńska, R. Chulist, A. Korneva, P. Zięba Acta Mater. 195, 2020, 184–198.